## Slide 1
Deformation of Nam Ngum 2 concrete faced rockfill dam (CFRD)in Laos after construction
Dr. Warakorn Mairaing,
Chinoros Thongthumachat
GERD, Kasetsart University,
Bangkok, Thailand

## Slide 2: Contents
Introduction to NN2 Dam
Monitoring Instruments for NN2 Dam
Deformation of Dam Body
Deformation of Face Slab
Face Slab Joint Movements
Conclusion

## Slide 3
Face Slab
Foundation Grouting
Plinth and
Perimeter Joint
NN2 Dam Project Layout

## Slide 4
Dam Features

## Slide 5: Progression of CFRD after the 60’s compacted rock-fill techniques
(Cruz et al., 2009)
Nam Ngum2

## Slide 6: General Deformation Characteristics

## Slide 7
Coarser particles
NN2 Dam Section

## Slide 8
8
The dam construction
2006
Started on 2006
The river bed was cleaned and the foundation was improved before the commencement of embankment work
Dam body began to embank on February 2008
The embankment constructed within 20 months
Feb 2008 – Nov 2009
The main dam embankment has mainly divided into 5 sequences.
The compacted sandstone rockfill has been controlled to achieve the dry unit weight more than 21.5 kN/m3 and the maximum of void ratio 0.20.
The 0.80 m lift thickness of 3B and 3C material has been employed depending on the maximum size of rockfill material.
 ≥ 21.5 kN/m3
emax= 0.2
0.80 m lift thickness
Sequence 1 consists of Zone 3B and 3D
The actual placement commenced on March 2008 of 10 m height start from downstream and left about 30 m at upstream path for construct the plinth at river bed.
March 2008
Sequence 2 started from April 2008 to January 2009, about 10 months.
The placement of rockfill on the upstream was done up to elevation 315 m asl, which corresponds to 115m in height.
April 2008 - January 2009, about 10 months.
El. + 315 m asl
115m
February - June 2009, about 5 months
1st stage of face slab
Sequence 3 had to construct parallel with the first stage of face slab construction. Started from February to June 2009, about 5 months
Then started the Sequence 5, the second stage face slab started commencement in December 2009 parallel with the earthfill and random fill placed on upstream face over the lower part of the face slab, Zone 1A and 1B, have also been compacted.
After completion of the second stage face slab and the wave wall, the last portion of embankment above the wave wall foundation was constructed
2nd stage of face slab
Sequence 4 after completion of the first stage concrete face slab then start compacted the embankment till the elevation reach to the wave wall foundation. The work took about 5 months started from July to November 2009.
July to November 2009, about 5 months
After Panarat K. (2011)
Notes: 8
8
The construction project was started on 2006.
The river bed was cleaned and the foundation was improved before the commencement of embankment work.
Dam body began to embank on February 2008.
The embankment constructed within 20 months.
The main dam embankment has mainly divided into 5 sequences.

## Slide 9: Summary of dam instruments in NN2 Dam
______________________________________________________________________________________________________
Instrumentation Notation Quantity Location
_______________________________________________________________________________________
Surface Monuments SM 14 Rockfill Upstream slope
21 Dam crest and Downstream slope
Inclinometer PI 3 sets Rockfill Downstream berm
Magnetic Settlement Gauge SG 41
Hydrostatic Settlement Cell HSC 22 Rockfill Section 2-4
Fixed Embankment Extensometer FEE 111 Rockfill Section 2-4
Total Earth Pressure Cell TPC 3 Rockfill Section 3
Strong Motion Accelerometer SMA 3 Rockfill Crest, downstream berm and abutment
Weather Station WS 1 set Rockfill Abutment
V-notch Measuring Weir VW 1 Rockfill Downstream toe
Open Standpipe Piezometer OSP 7 Rockfill Downstream of abutment and dam toe
Inclined Iinclinometer IIC 1 Face slab Section 3
Electro Level (Tilt Meter) EL 23 Face slab Section 1-4
1 Dimensional Joint Meter JM 4 set Face slab Parapet wall - face slab
2 Dimensional Joint Meter 2JM 10 set Face slab Between vertical joint
3 D (Perimetric) Joint Meter PJM 13 set Face slab Along perimetric - construction joint
3D Concrete Strain Gauge TSG 27 set Face slab Within concrete slab
Rebar Strain Gauge RBSG 27 Face slab Within concrete slab
Non Stress Strain Meter RBSG 7 Face slab Beneath concrete slab
Distributed Fiber Optic Temperature DFOT 900 m Plinth Beneath concrete slab
Vibrating Wire Piezometer VWP 35 Dam foundation
______________________________________________________________________________________________________
411 sensors
Notes: There are several kinds of dam instrument on NN2 dam and about 485 sensors were installed within dam body and on the face slab.
-
Some instruments had been installed in dam foundation before filling of the dam embankment.

## Slide 10
(TILTMETER)

## Slide 11
Tiltmeter
Embankment
Extensometer

## Slide 12
Construction and
Dam Operation
Timelines
3 years

## Slide 13: Lateral Displacement on Plan View
Max. at SDP 6.5
Dis. = 150 mm.
SECTION A
SECTION B
SECTION C
SECTION D
SECTION E
December 2012

## Slide 14: Displacement on Longitudinal Plane
Chart: 
| 433.93099999999998 | 433.90139365208643 | 431.84017225377414 | 432.33927810529838 | 431.49235765564714 | 431.01555583044114 | 430.6791615963316 | 430.5150195809519 | #N/A | 429.88703091329239 | 429.25549175190372 | 428.37112246432145 | 428.79397157267795 | 428.37450353511662 | 428.82856744769816 | 427.60305559052438 | 428.03706686900654 | 427.95957110108168 | 428.19474839942393 | 428.42113159949781 | 427.25059409623225 | 427.87054689665757 | 426.42363879085383 | 427.63479600087044 | 425.74410053033102 | 425.91825956577901 | 426.27937108937897 | 426.36128416789239 | 427.20750415142459 | 426.88482494027397 | 426.00628335555587 | 427.2039848188092 | 425.19385483743076 | 425.20329998798081 | 427.09894915585619 | 425.29212809200271 | 424.40654133170307 | 424.43845990623879 | 423.76871671499839 | 424.24802792599058 | 425.44999033556479 | 424.80181832916043
SDP6.1 | 374.173 | 373.373 | 373.373 | 373.373 | 372.973 | 372.173 | 372.173 | 371.773 | 370.973 | 370.773 | 370.173 | 369.373 | 369.173 | 369.173 | 368.973 | 368.573 | 368.573 | 367.973 | 367.973 | 367.973 | 367.173 | 366.973 | 366.773 | 366.773 | 366.573 | 366.573 | 366.373 | 366.173 | 365.773 | 365.573 | 365.373 | 364.973 | 364.973 | 364.173 | 364.173 | 363.773 | 363.573 | 363.173 | 363.173 | 363.173 | 362.773 | 362.773
SDP6.2 | 373.927 | 373.327 | 373.127 | 373.127 | 371.527 | 370.127 | 369.527 | 368.327 | 366.927 | 366.127 | 365.127 | 364.727 | 364.127 | 363.527 | 362.927 | 362.527 | 362.127 | 361.927 | 360.927 | 360.927 | 360.127 | 359.127 | 358.527 | 358.527 | 357.927 | 357.527 | 356.927 | 356.727 | 356.127 | 355.927 | 355.327 | 355.127 | 354.927 | 353.527 | 353.327 | 352.527 | 352.127 | 351.327 | 351.127 | 351.127 | 350.727 | 350.527
SDP6.3 | 373.667 | 373.067 | 372.467 | 372.267 | 369.467 | 367.267 | 366.667 | 364.667 | 362.867 | 362.267 | 360.667 | 359.667 | 358.667 | 358.467 | 357.067 | 356.267 | 355.867 | 355.467 | 354.067 | 353.467 | 352.067 | 351.267 | 350.467 | 350.467 | 349.867 | 349.067 | 348.667 | 348.467 | 347.867 | 347.467 | 346.467 | 346.267 | 345.867 | 344.267 | 343.667 | 342.867 | 342.267 | 341.267 | 340.867 | 340.667 | 340.267 | 340.067
SDP6.4 | 373.636 | 372.836 | 371.836 | 370.636 | 367.636 | 367.436 | 366.436 | 364.236 | 362.636 | 361.836 | 360.036 | 358.836 | 357.636 | 357.036 | 356.036 | 354.836 | 354.436 | 354.036 | 352.236 | 351.436 | 350.036 | 349.036 | 348.236 | 348.036 | 347.236 | 346.836 | 346.036 | 345.836 | 345.236 | 344.836 | 344.036 | 343.636 | 343.036 | 341.436 | 340.836 | 339.836 | 339.036 | 338.036 | 337.836 | 337.236 | 337.036 | 336.636
SDP6.5 | 374.022 | 372.022 | 371.822 | 370.222 | 367.422 | 365.022 | 363.422 | 361.622 | 360.022 | 358.622 | 357.422 | 355.822 | 355.022 | 354.822 | 353.222 | 352.222 | 352.222 | 351.422 | 349.622 | 348.822 | 347.622 | 346.422 | 345.822 | 345.622 | 345.022 | 344.222 | 343.422 | 342.822 | 342.422 | 342.022 | 341.022 | 340.422 | 339.822 | 338.422 | 337.422 | 336.622 | 334.622 | 333.622 | 333.222 | 332.622 | 332.422 | 332.022
SDP6.6 | 373.925 | 372.525 | 372.125 | 370.725 | 367.925 | 365.925 | 364.325 | 362.925 | 361.325 | 360.125 | 358.925 | 357.725 | 356.925 | 356.325 | 355.325 | 354.525 | 354.525 | 353.525 | 352.125 | 351.125 | 349.925 | 348.925 | 348.325 | 347.925 | 347.325 | 346.525 | 346.125 | 345.925 | 345.325 | 344.925 | 343.925 | 343.325 | 342.725 | 341.525 | 340.725 | 339.725 | 338.725 | 337.925 | 337.525 | 337.325 | 336.925 | 336.925
SDP6.7 | 373.904 | 372.904 | 372.704 | 371.704 | 369.704 | 367.904 | 367.104 | 365.704 | 364.504 | 363.704 | 362.504 | 361.304 | 360.304 | 359.904 | 357.704 | 356.704 | 356.104 | 355.704 | 354.304 | 353.304 | 352.504 | 351.704 | 350.904 | 350.704 | 350.104 | 349.504 | 349.104 | 348.704 | 348.104 | 347.704 | 346.904 | 346.504 | 346.104 | 344.904 | 344.304 | 343.504 | 342.704 | 341.904 | 341.504 | 341.104 | 340.904 | 340.704
SDP6.8 | 373.825 | 373.625 | 373.625 | 373.425 | 372.425 | 371.625 | 370.625 | 370.225 | 369.025 | 369.025 | 368.425 | 367.625 | 367.425 | 366.825 | 366.225 | 366.025 | 366.025 | 365.825 | 365.225 | 364.425 | 364.025 | 363.025 | 362.425 | 362.425 | 362.025 | 361.425 | 361.225 | 361.025 | 360.425 | 360.225 | 359.625 | 359.425 | 359.025 | 358.425 | 358.025 | 357.425 | 357.025 | 356.425 | 356.225 | 356.225 | 356.025 | 355.825
SDP6.9 | 374.157 | 373.957 | 373.957 | 373.757 | 373.557 | 373.557 | 373.357 | 373.357 | 373.157 | 373.157 | 372.957 | 372.957 | 372.957 | 372.757 | 372.557 | 372.557 | 372.557 | 372.557 | 372.557 | 372.357
Maximum incremental displacement for last 2 months, at SDP 6.3
Dis. = 8 mm.
Section A
Section B
Section C
Section E
5
5
6
8
6
2
6
3
2
1
3
4
3
1
0
0
3
1
2
3
4.0 mm/mo
Max. at SDP 6.5
Dis. = 246 mm.
Section A
Section B
Section C
Section D
Section E
199
246
222
200
140
69
221
110
14
133
175
160
103
157
39
25
22
14
39
31
Looking upstream
18 DEC 12
Section D
Accumulative
Last 3 months

## Slide 15: Displacements on Transverse Sections
Chart: Offset distance (m)
| 15.191000000000001 | 14.738054000101226 | 15.133815562737892 | 15.230355720590151 | 17.048171603395218 | 18.26745538811856 | 19.483629269713305 | 20.413674887355263 | #N/A | 21.160087342308614 | 21.757082723540712 | 23.228172526326983 | 23.886676241310191 | 24.941117210608056 | 24.678840169601433 | 25.749460551574241 | 25.211852909808123 | 26.744777904344609 | 28.127793748407086 | 28.560811258060934 | 29.418233545632887 | 30.631179402102248 | 30.164031708675935 | 31.422673237636893 | 31.939312411798731 | 32.293669150563048 | 32.116654982745985 | 32.244021525519081 | 31.446575467999779 | 31.705916231115225 | 33.355401452906101 | 32.371517350764165 | 33.383623685717936 | 34.824206878454746 | 36.051753115584894 | 35.906280183135756 | 35.969437848382938 | 37.894076606181926 | 37.657188912000017 | 37.654165773814825 | 38.06019600295857 | 38.978800798879242 | 37.179865396101931 | 38.108681827101599 | 39.050763951777355 | 38.661881767578308 | 39.270418179842103 | 39.04383942040841 | 39.215142356453534 | 38.391287871343359 | 38.820556549346158 | 37.960939079552816 | 38.513601132326954 | 37.539503182204641 | 38.428985472659932
SDP6.6 | 373.925 | 372.525 | 372.125 | 370.725 | 367.925 | 365.925 | 364.325 | 362.925 | 361.325 | 360.125 | 358.925 | 357.725 | 356.925 | 356.325 | 355.325 | 354.525 | 354.525 | 353.525 | 352.125 | 351.125 | 349.925 | 348.925 | 348.325 | 347.925 | 347.325 | 346.525 | 346.125 | 345.925 | 345.325 | 344.925 | 343.925 | 343.325 | 342.725 | 341.525 | 340.725 | 339.725 | 338.725 | 337.925 | 337.525 | 337.325 | 336.925 | 336.925 | 336.125 | 335.725 | 335.725 | 335.325 | 335.125 | 334.525 | 334.525 | 334.125 | 334.125 | 333.725 | 333.525 | 333.325 | 332.925
Chart: Offset distance (m)
| -5.0486606275654351 | -3.0990201055483837 | -3.304348418930013 | -3.0990453709864738 | -2.8304636202024795 | -1.758382009967915 | -1.5076971644382571 | -2.079070579272408 | -1.9171628638560998 | -1.3532396382936778 | -1.9643033162300676 | -1.4144149006964741 | -1.5177072625521344 | -0.77257539627506322 | 0.37478517927349664 | 1.0206425157871246 | 2.2282634661593477 | 2.6873565024468169 | 3.2938140757697214 | 3.3959251079278197 | 3.8717594164552365 | 3.8872853444737405 | 4.5163734778309044 | 4.2049604398689988 | 5.5151415018805094 | 5.4003856496414899 | 5.0796260256179488 | 5.3724622792885297 | 5.7791183012656768 | 4.8215717102071016 | 4.6769781691958636 | 3.8379336220259095 | 4.6750716056189168 | 4.7383389186674334 | 4.7153896708189018 | 4.5078411697988114 | 4.5283106258688042 | 5.3357241447802339
D03 | 383.443 | 380.843 | 380.243 | 379.643 | 378.843 | 377.843 | 377.243 | 376.443 | 375.843 | 375.643 | 375.643 | 375.243 | 374.843 | 374.043 | 373.043 | 372.443 | 371.443 | 370.243 | 369.043 | 368.443 | 368.043 | 367.443 | 367.243 | 366.443 | 366.243 | 365.843 | 365.443 | 365.243 | 364.843 | 364.843 | 364.643 | 364.643 | 364.643 | 364.443 | 364.443 | 364.443 | 364.443 | 364.243
SDP6.5 | 374.022 | 372.022 | 371.822 | 370.222 | 367.422 | 365.022 | 363.422 | 361.622 | 360.022 | 358.622 | 357.422 | 355.822 | 355.022 | 354.822 | 353.222 | 352.222 | 352.222 | 351.422 | 349.622 | 348.822 | 347.622 | 346.422 | 345.822 | 345.622 | 345.022 | 344.222 | 343.422 | 342.822 | 342.422 | 342.022 | 341.022 | 340.422 | 339.822 | 338.422 | 337.422 | 336.622 | 334.622 | 333.622 | 333.222 | 332.622 | 332.422 | 332.022 | 331.422 | 331.022 | 330.822 | 330.422 | 330.422 | 329.822 | 329.822 | 329.422 | 329.422 | 329.022 | 328.822 | 328.622 | 328.222
Dis. at SDP 6.6
Mar = 153 mm.
Jun = 167 mm.
Sep = 200 mm.
Dec = 220 mm.
Apr = 230 mm.
Jul = 236 mm.
Oct = 248 mm.
Dec = 254 mm.
Dis. at SDP 6.5
Mar = 168 mm.
June = 186 mm.
Sep = 223 mm.
Dec = 253 mm.
Apr = 261 mm.
Jul = 266 mm.
Oct = 281 mm.
Dec = 287 mm.
Section C
Section D
Right Abutment
Maximum Section

## Slide 16: Movement of Dam Surface
Chart: Date
SDP6.9 | 0 | 8.8658 | 7.1586 | 8.3215 | 8.5725 | 8.2499 | 10.205 | 11.2671 | 11.2663 | 14.4755 | 5.1637 | 9.8587 | 14.1947 | 11.9328 | 10.37 | 10.3935 | 9.5151 | 14.0231 | 15.7783 | 13.7402 | 5.2577 | 13.7519 | 7.3686 | 13.0799 | 15.8094 | 15.4023 | 18.6453 | 9.4142 | 7.1535 | 10.3424 | 17.774 | 10.7444 | 14.0485 | 5.3865 | 7.9229 | 11.8079 | 12.2308 | 11.3973 | 13.9024 | 13.8454 | 8.2559 | 13.4723 | 13.2139 | 11.8495
Construction
Start Impounding
2nd full filling
Haima 2011
Along dam axis displacement with time
1st full filling
3rd full filling
R
L

## Slide 17: US/DS displacement with time
Chart: Date
SDP6.9 | 0 | 1.6341 | 1.121 | 1.8893 | 2.3075 | 4.3741 | -3.7351 | -0.098993 | 0.49075 | 0.32804 | -0.46539 | -0.26366 | 2.9004 | -0.6041 | 2.2192 | 4.9011 | 4.0268 | 0.61237 | 0.09783 | 4.8316 | 3.0212 | 4.0363 | 8.25 | 4.4817 | 3.9766 | 3.45 | 3.5682 | 6.6092 | 12.2324 | 3.2401 | 4.3564 | 4.2949 | 6.2009 | 6.2542 | 4.7217 | 4.6216 | 5.426 | 7.7375 | 5.9977 | 5.9994 | 10.8719 | 9.1337 | 4.4906 | 5.2762
Finishing Works
Start Impounding
1st full filling
Haima 2011
2nd full filling
3rd full filling
+314
+373
+257
Crest

## Slide 18: Settlement rates
Chart: Date
SDP6.9 | 0 | -1 | -1 | -2 | -3 | -3 | -4 | -4 | -5 | -5 | -6 | -6 | -6 | -7 | -8 | -8 | -8 | -8 | -8 | -9 | -8 | -9 | -9 | -9 | -9 | -10 | -10 | -11 | -11 | -11 | -11 | -11 | -11 | -11 | -11 | -11 | -12 | -12 | -12 | -12 | -13 | -13 | -13 | -14
Chart: Date
SDP6.9 | 0 | -2.1429 | -1.0714 | -0.90226 | -1.6917 | -1.0714 | -1.0714 | -1.1243 | -0.91054 | -0.91054 | -1.267 | -0.90538 | 0 | -1.0222 | -2.1429 | -0.78947 | 0 | 0 | 0 | -1.1465 | 0.1633 | -0.027675 | -0.92466 | 0 | 0 | -1.0714 | -1.0714 | -0.90226 | -0.90226 | -6.0904e-11 | 0 | 6.0904e-11 | 0 | 0 | 0 | 0 | -1.0714 | -0.78947 | 0 | 0 | -1.0714 | -1.0714 | 1.3513e-12 | -1.0441
Total Settlement
Settlement Rate
It is obvious that the settlement was induced slower by the 3rd filling.
First filling
Second filling
Smaller than 5.0 mm./month
Third filling
Finishing Period
Finishing Period
Construction Period

## Slide 19
Chart: Time (days after impounding started)
Creep parameters decrease with time and related to the water level.
= 0.05-0.25 for medium strength rockfill
(Hunter et.al., 2003)
Chart: Time (days after impounding started)
= 0.15-0.4 % in 10 Yrs for medium strength rockfill
(Hunter et al, 2003)
-0.02
-0.04
-0.06
-0.08
-0.10
-0.12
-0.14

## Slide 20: Crest Settlement in literatures
Post construction total crest settlement and long-term creep rate for CFRDs
(Hunter et al, 2003)
Rockfill Classification | Total Post Construction Settlement (% of dam height) |  | Long-term Creep Rate, ** (% /log cycle)
 | 10 years | 30 years | 
Dumped Rockfill | 0.6 to 1.0 | 1.0 to 1.5 | 0.3 to 1.5
Well Compacted Rockfills: |  |  | 
- Medium to high strength* | 0.15 to 0.4 | - | 0.05 to 0.25
- Very high strength, quarried* | 0.06 to 0.2 | - | 0.02 to 0.10
- Gravel Rockfills | 0.2 to <0.05 | - | <0.10
Note:
* Rock substance unconfined compressive strength medium 6 to 20 MPa, high 20 to 70 MPa, very high 70 to 240 MPa.
** %strain =  (log T2 – log T1)
0.15 – 0.20
a < 0.10 For last filling
Notes: 20

## Slide 21: Relation of crest settlement and leakage
%Settlement and possibility of leakage
Statistical data summarized by Hunter and Fell (2005) and GERD (2013)
0
5
10
15
20
25
30
35
0.1
0.4
0.6
0.9
1.1
1.3
1.6
1.8
2.1
%
0.00
0.05
0.10
0.15
0.20
0.25
0.30
0.35
0
5
10
15
20
25
30
35
0.1
0.4
0.6
0.9
1.1
1.3
1.6
1.8
2.1
%
Crest Settlement
Frequency
0.00
0.05
0.10
0.15
0.20
0.25
0.30
0.35
Probability Density
Almost certainly leak
Possible some leakage
0.15% at Present
0.20-0.25% for 10 yrs.

## Slide 22
Deformation of Face Slab

## Slide 23
Face slab Deflection Instruments
Section 1 Ch. 372
Section 2 Ch. 272
Section 3 Ch. 172
Section 4 Ch. 72
1.1 2.1 3.1 4.1
1.2 2.2 3.2 4.2
1.3 2.3 3.3 4.3
2.4 3.4 4.4
2.5 3.5 4.5
2.6 3.6 4.6
3.7
3.8
3.9
Electro Level (EL)
3D joint meter (TJM)
1st stage of face slab
2nd stage of face slab
Face slab layout
TJM
TJM
EL
EL
Section of dam
Notes: 23
Electro Level were used for monitoring changes in rotation at the surface of face slab which interpreted with 3D joint meters.
TJMs measurement the joint movement between face slab and plinth and also between 1st and 2nd stage face slab.
The face slab deflections were interpret at 4 section.
23

## Slide 24: Deflection of face slab
Section 1
Section 2
Section 3
Section 4
The concrete face slab has the deflect more than last 3 months still related to the RWL.
Max. =51 cm.
Max. =43 cm.
As of Jan 2013
Max. =30 cm.
Max. =35 cm.
Dam Crest
U/SToe
U/SToe
U/SToe
U/SToe

## Slide 25: Predicted Deflections from Design
LC1. Reservoir (Empty)
LC2. Reservoir (MoL)
LC3. Reservoir (FSL)
LC4. Reservoir (PMF)
Max = 0.0401 m
Max = 0.457 m
Max = 0.474 m
Max = 0.323 m
Notes: 25

## Slide 26
Contours of face slab deflection (in mm) during first impounding.
18 Nov 2010
18 Dec 2010
18 Oct 2010
WL +368
WL +370
WL +370
18 Feb 2011
WL +371
18 Jan 2011
WL +371
18 Mar 2011
WL +371
-350 mm
-430 mm
-460 mm
-480 mm

## Slide 27
Face Slab Joint Movement

## Slide 28: Location of Jointmeters (1D, 2D, 3D)
Looking downstream
3D Jointmeter 6 sets
2D Jointmeter (add.) 8 sets
1D Jointmeter 4 sets
Perimetric Joint
Horizontal Construction Joint +285
3D Jointmeter (add.) 7 sets
Notes: 28
fdsfiek

## Slide 29: Perimeter Joint Details
Plinth Wall
Face Slab
Plinth Wall
Face Slab
Flexibility > 15 cm.

## Slide 30: Three Direction (Perimetric) Jointmeter (TJM)
Perpendicular
Parallel
Perpendicular
Sign Notation: Movement of face concrete related to plinth
X (Perpendicular) direction
  + Opening, - Closing
Y (Parallel) direction
  + Toward to LA, - Toward to RA
Z (Settlement) direction
  + Upward, - Downward
Z
X
Y
Notes: 30

## Slide 31: Joints Monitoring vs. Time
Chart: Date
SDP6.9 | 0 | 1.6341 | 1.121 | 1.8893 | 2.3075 | 4.3741 | -3.7351 | -0.098993 | 0.49075 | 0.32804 | -0.46539 | -0.26366 | 2.9004 | -0.6041 | 2.2192 | 4.9011 | 4.0268 | 0.61237 | 0.09783 | 4.8316 | 3.0212 | 4.0363 | 8.25 | 4.4817 | 3.9766 | 3.45 | 3.5682 | 6.6092 | 12.2324 | 3.2401 | 4.3564 | 4.2949 | 6.2009 | 6.2542 | 4.7217 | 4.6216 | 5.426 | 7.7375 | 5.9977 | 5.9994 | 10.8719 | 9.1337 | 4.4906 | 5.2762
Construction
Start Impounding
1st full filling
Haima 2011
2nd full filling
3rd full filling
+314
+373
+257
Crest
1
2
3
4
5
6

## Slide 32: Movement of Joints in May 10
Sign Notation: Movement of face concrete related to plinth
X (Perpendicular) direction Y (Parallel) direction Z (Settlement) direction
+ Opening, - Closing + Toward to LT, - Toward to RT + Upward, - Downward
Joint Closing
Joint Settlement
Joint Sliding
1st Filling
1

## Slide 33: Movement of Joints in October 10
Sign Notation: Movement of face concrete related to plinth
X (Perpendicular) direction Y (Parallel) direction Z (Settlement) direction
+ Opening, - Closing + Toward to LT, - Toward to RT + Upward, - Downward
Joint Closing
Joint Settlement
Joint Sliding
1st Filling
2

## Slide 34: Movement of Joints in June 11
Sign Notation: Movement of face concrete related to plinth
X (Perpendicular) direction Y (Parallel) direction Z (Settlement) direction
+ Opening, - Closing + Toward to LT, - Toward to RT + Upward, - Downward
2JM5.1 malfunction
Joint Closing
Joint Settlement
Joint Sliding
1st Filling
3

## Slide 35: Movement of Joints in October 11
Sign Notation: Movement of face concrete related to plinth
X (Perpendicular) direction Y (Parallel) direction Z (Settlement) direction
+ Opening, - Closing + Toward to LT, - Toward to RT + Upward, - Downward
Joint Closing
Joint Settlement
Joint Sliding
2nd Filling
4

## Slide 36: Movement of Joints in July 12
Sign Notation: Movement of face concrete related to plinth
X (Perpendicular) direction Y (Parallel) direction Z (Settlement) direction
+ Opening, - Closing + Toward to LT, - Toward to RT + Upward, - Downward
2JM5.8 fluctuated presumed fail
2JM5.2 fluctuated presumed fail
2JM5.1 fluctuated presumed fail
Joint Closing
Joint Settlement
Joint Sliding
3rd Filling
5

## Slide 37: Movement of Joints in January 13
Sign Notation: Movement of face concrete related to plinth
X (Perpendicular) direction Y (Parallel) direction Z (Settlement) direction
+ Opening, - Closing + Toward to LT, - Toward to RT + Upward, - Downward
Joint Closing
Joint Settlement
Joint Sliding
3rd Filling
6

## Slide 38: Rate of displacement at TJM 2.2
Sign Notation: Movement of face concrete related to plinth
X (Perpendicular) direction
+ Opening, - Closing
Y (Parallel) direction
+ Toward to LT, - Toward to RT
Z (Settlement) direction
+ Upward, - Downward
The joints have rate of movement increasing during first impounding (Jun to Aug 2010), then decreasing after fully impounding (Aug 2010 to Mar 2011) and then nearly to constant.
After 2nd impounding in Jul 2011, the rate of settlement slightly increased .
TJM 2.2
Chart: Date of Reading
 | 100 | -100
Chart: Date of Reading
 | 100 | -100
Displacement
Rate of Displacement
1st Filling
2nd Filling
2010
2011
settlement

## Slide 39: Overall Relative Face Slab Movement
Focal Points

## Slide 40: Conclusion
NN2 Dam in Laos PDR is a 182 m. high and one of the major CFRD in the world. The Thai investors was initiated and carried on this hydropower project. Thus the knowledge of dam behavior is very important not only for dam safety, O&M but also for the engineers to handle the future design and construction.
The deformation of CFRD during construction and initial stage of impounding is related to the leakage through dam. The integrity and water tightness of the face slab can also evaluate by the monitoring of face slab deflection and joint movements.
The maximum settlement of dam crest during 3 years of reservoir operation was 24.6 cm. or 0.15 % of dam height. This dam crest settlement is well below the critical deformation of 0.4 to 1.0% of dam height that can cause some crack on the face slab.

## Slide 41: Conclusion (cont.)
During first impounding, the water level reach to +371 m asl, the maximum face slab deflection was 486 mm. as comparing to the anticipated deflection from the design analysis is of 457 mm. The contour of slab deflection indicated the maximum deflection occurring at approximately mid height on the deepest section.
The local maximum face slab settlement of 80 mm. was recorded at the beginning of the 1st impounding. This rate was slowed down after the first impounding and the settlement was still in the allowance of copper water stop and joint sealing.

## Slide 42: Thank you for your attention